## Slide 1
Construction Workers and Nanomaterials: Perspective of Vulnerable and Unique Stakeholders
Session D: Emerging Techologies and Advanced Materials
QEEN II, October 9, 2018
Bruce Lippy, Ph.D., CIH, CSP
Director of Safety Research, CPWR
Gavin West, MPH
Analyst, CPWR
Notes: Trainer Notes
Photo of construction worker courtesy of Kiewit Power Constructors.
Thank you. I greatly appreciate the opportunity to speak to this conference. It is wonderful to be in Denver. When you come from Baltimore, every place is up, but being in the shadow of the Rockies is always exhilarating.

## Slide 2: Here are the questions I’d like to tackle:
Why are construction workers particularly vulnerable stakeholders?
What can we say about construction workers’ exposure to engineered nanomaterials?
What are we doing to understand the hazard posed by construction nanomaterials?
How are we doing communicating risk to construction workers?
Notes: What are the concerns about nanomaterials in construction?
What is the state of hazard communication around nanomaterials?
How informed are workers about risk?
How should workers be trained about nanomaterials?

## Slide 3: Why are construction workers particularly vulnerable stakeholders?
Question 1
1
Notes: Improvements nano-enabled products will bring to construction

## Slide 4: Construction is dominated by small employers and a diverse workforce
90% have <20 employees
About 80% have <10 employees
30% of workers are Hispanic
14% are employed by temp agencies
Sources: U.S Census Bureau; CPWR Construction Chart Book 5th Edition; CPWR 2nd Quarter 2015 Quarterly Data Report
Notes: Construction is dominated by small employers and a diverse workforce. About 90% of construction establishments employ less than 20 employees – and roughly 80% employ less than 10 workers.
Like other small business, many of these contractors have limited resources and have low profit margins and are under-resourced.
Small contractors are more likely to hire workers considered at a greater risk for injury [including young workers, people who are less educated, and immigrants - Belman and Levine 2004; NIOSH Overlapping Vulnerabilities]. [According to Bloomberg Businessweek, non-residential construction companies earned only a 0.78 percent profit margin in 2010. http://smallbusiness.chron.com/factors-affect-percentage-profit-margins-construction-35114.html
About 30% of construction workers are Hispanic and 14% are employed by temporary agencies, which adds new complexity to who is responsible for training these workers.

## Slide 5: Small firms represent a disproportionate percentage of construction fatalities (2015)
Chart: 
| 100+ employees | 20-99 employees | 1-19 employees
Employment | 0.2894 | 0.3355 | 0.3751
Fatalities | 0.16718 | 0.26316 | 0.56966
CPWR The Construction Chart Book 2018
Notes: Small firms represent a disproportionate percentage of construction fatalities. This is 2015 data from our Chart Book. Note that firms with 1-19 employees represented a bit over one-third of the construction firms, but over half of the fatalities (in red). In contrast, firms with 100 or more employees represented 28.9% of companies, but only 16.7%. This is a major challenge we face. The small firms have the greatest need for support and information, but are the hardest to reach.

## Slide 6: In 2010, more than half of U.S. construction workers reported exposure to vapors, gas, dust or fumes twice a week or more
Liss GM, Petsonk EL, Linch KD [2010, Nov]. The construction industry. In: Occupational and Environmental Lung Diseases
Photo
credit:
Bruce
Lippy
Notes: In 2010, more than half of construction workers reported exposure to vapors, gas, dust or fumes twice a week or more.
NOTES:
In 2010, more than 50 percent of construction workers reported that they were regularly exposed to vapors, gas, dust or fumes at work twice a week or more, which was more than double that of all industries combined. Construction workers, representing only five to six percent of the non-farm labor force, account for half of all occupational cancers. CPWR, The Center for Construction Research and Training. [2013, April]. The construction chart book. Online. Available at: http://www.cpwr.com. p. 35.
Liss GM, Petsonk EL, Linch KD [2010, Nov]. The construction industry. In: Occupational and Environmental Lung Diseases: Diseases from Work, Home, Outdoor, and Other Exposures. Eds: Tarlo S, Cullinan P, & Nemery B, eds., Hoboken, NJ: John Wiley & Sons, Ltd. 273-289.

## Slide 7: Bystander exposures can be significant in construction
Photo courtesy of the NJ Department of Health and Senior Services' NIOSH-funded Silicosis Surveillance Project

## Slide 8: What can we say about construction workers’ exposure to engineered nanomaterials?
Question 2
1
2
Notes: What is the current state of hazard communication for nano?

## Slide 9: Multiple studies have evaluated release of ENPs from coatings during sanding (Dylla and Hassan, 2012; Vaquero, Gelarza and Ipina, 2015; West et al. 2016)
“Results are mostly encouraging with regard to worker health.”
Notes: From JOEH-accepted draft: Only a relatively small number of studies have examined release of nano-TiO2 from construction. Most of these studies investigated sanding of paints or coatings,(5-9) while just a few examined initial spray application of coatings or machining of cementitious materials.(10-12) Results from these studies are mostly encouraging with regard to worker health, but further research is needed to bolster the current understanding of exposure risk among construction workers handling NEPs, an area of knowledge that remains fairly limited.
Dylla, H. and M.M. Hassan: Characterization of nanoparticles released during construction of photocatalytic pavements using engineered nanoparticles. J. Nanopart. Res. 14(4):1-15 (2012). Vaquero, C., N. Gelarza, J.L. López de Ipiña, et al.: Occupational exposure to nano- TiO2 in the life cycle steps of new depollutant mortars used in construction. J. Phys. : Conf. Ser. 617(1):012006 (2015). West, G.H., B.E. Lippy, M.R. Cooper, et al.: Toward responsible development and effective risk management of nano-enabled products in the U.S. construction industry. J. Nanopart. Res. 18(2):49 (2016).

## Slide 10: April 2017, we sampled exposures during spraying paint containing nano titanium dioxide, with subsequent sanding
Notes: Photomicrograph at 100,000x

## Slide 11: We used the same 3-pronged sampling approach
Prong 1: Real-time instruments
TSI Scanning Mobility Particle Sizer and Optical Particle Sizer
Photo courtesy Earl Dotter

## Slide 12: Prong 2: standard industrial hygiene sampling for dust and metals
Photos courtesy Earl Dotter

## Slide 13: Prong 3: electron microscopy of bulk and airborne particles
SEM bulk characterization of paint
Sonicated in water
Sonicated in acetone
Conventional paint in acetone
Notes: Bulk characterization via SEM showing nano-enabled paint prepared in water (left), the nano-enabled paint prepared in acetone (middle), and a conventional comparison paint prepared in acetone (right)

## Slide 14: We used an environmental chamber with HEPA-filtered air
Vacuum

## Slide 15: We sprayed and then sanded plywood sheets
LEV
Notes: The coated boards were allowed to dry overnight although the manufacturer of the Defy indicates drying time is one hour. The next day the test subject sanded boards, both coated and uncoated (as controls), using a DeWalt 5-inch random orbital sander. Controls were provided with a Hilti vacuum as an LEV or the collection bag that came with the sander. The team used a TSI Scanning Mobility Particle Size to count and size particles generated during the work.

## Slide 16: We again demonstrated local exhaust can significantly reduce nanoparticle release
Particles per cubic centimeter of air
dN/dlogDp (#/cm^3)
Coated, LEV
Uncoated, LEV
Coated, Bag filter
Uncoated, bag filter
Notes: Figure 8. Comparison of airborne nanoparticle concentrations while sanding coated or uncoated boards with either LEV or a dust collection bag: Center lines show the medians; box limits indicate the 25th and 75th percentiles as determined by R software; whiskers extend 1.5 times the interquartile range from the 25th and 75th percentiles, outliers are represented by dots; width of the boxes is proportional to the square root of the sample size. n = 22, 22, 21, 22 sample points. The notches are defined as +/-1.58*IQR/sqrt(n) and represent the 95% confidence interval for each median. Non-overlapping notches give roughly 95% confidence that two medians differ.

## Slide 17: “This study may be the first to provide evidence suggesting potential for overexposure to nano-TiO2 during routine construction activity in reference to the NIOSH REL for ultrafine TiO2 (0.3 mg/m3 as a 10-hour TWA)”
West et al., draft manuscript

## Slide 18: What are we doing to understand the hazard posed by construction nanomaterials?
Question 3
1
2
3
Notes: Uniqueness of construction work

## Slide 19: Our site currently features 583 commercial construction products reported to be nano-enabled and 265 articles
www.nano.elcosh.org
Notes: Our site, housed within CPWR’s electronic library of occupational safety and health, known as elcosh, currently contains 583 commercial construction products reported to be nano-enabled.
The phrase ‘reported to be nano-enabled’ may have caught your attention, and this is an important point.
The site plainly states that we do not have proof of the presence of nanoparticles in these products; only a reasonable belief the product may be nano-enabled.
Currently in the United States, there are no labelling requirements for engineered nanomaterials used in construction products.
As a result, our inventory cannot be comprehensive, and there is little practical recourse for researchers or contractors to determine if a given product does in fact contain engineered nanomaterials.
Some construction products marketed as ‘nano’ do not contain nanomaterials, and some companies may not convey that engineered nanomaterials are used in their products.
Our website does illustrate which nanomaterials are reported to be used in different construction applications, improving our understanding of where and what types of exposures might occur.
Let’s have a look.
(GO TO WEBSITE)
This is the elcosh home page and the link to our inventory is here (CLICK).
It is a straightforward website with two main components – product entries and a section for informational resources.
Recently added products are featured on the home page.
We can click on one to learn more. (CLICK SEALER)
The description tells us that this sealer has a high-solids formulation and delivers exceptional abrasion resistance.
Numerous engineered nanomaterials, such as aluminum oxide nanoparticles, can be used to impart abrasion resistance, but our reason for inclusion states that this product features a proprietary nanotechnology.
In this case, we are unable to determine the types of nanoparticles that may be present, if at all.
This page also tells us that the product is made in the USA, the safety data sheet is available online, and that it is designed to be used on interior concrete.
While not explicitly stated, an astute practitioner can then infer where exposures might occur – during spray application, for example, or while refinishing the coated surface at a later date.
(BACK TO HOME PAGE)
Users can search for products or browse product categories.
A visitor to our site might notice that 96 coatings for mineral surfaces are featured on site and wish to learn more.
(CLICK COATINGS MINERAL THEN SCROLL SLOWLY)
Scrolling through this list, it becomes apparent that certain nanomaterials, such as nano-lithium, nano-silica, and nano-titanium dioxide are reportedly used in similar products and applications.
(STOP AT GRAF-X WB)
One might notice that this anti-graffiti coating, which is sold by Home Depot for $60 a gallon, reportedly contains multiple nanomaterials, including… and I quote: plexi acrylic nano fusion, which is listed on the safety data sheet.
(BACK TO HOME)
Additional resources can be accessed in the news and info portion of our website, which remains a work in progress
(CLICK NEWS)
Recent articles are displayed in the upper left.
Articles we wish to feature, such as the NIOSH current intelligence bulletins, are below, and users can browse remaining resources by topic. Most resources are classified under materials innovations or EHS.
(STOP SCREEN SHARE, GO BACK TO PPT)

## Slide 20: Paints and coatings still dominate
Chart: 
| Paints/coatings (57.5%) | Other* (19.6%) | Insulation (6.3%) | Coatings additives (4.7%) | Cement (4.7%) | Patching compounds (2.5%) | Roofing (2.5%) | Lubricants (2.3%)
Number of Products | 320 | 109 | 35 | 26 | 26 | 14 | 14 | 13
Draft Chart Book graphic (2a)
Notes: Paints and coatings still dominate
*Other includes surface preparation, thermal spray coating materials, adhesives, additives for concrete/cement, flooring, glass and solar panels, metal, weld overlays, drywall, miscellaneous, HV/AC, prepregs, weatherproofing membranes, additives for asphalt, caulking, joint sealants, lighting, lumber, boiler additives, fasteners, fuel additives, and interior design.
Note: Data are based on 557 products in the inventory as of July 7, 2017.
Source: eLCOSH Nano, Construction Nanomaterial Inventory (2017). www.nano.elcosh.org

## Slide 21: NIOSH collected aerosol samples of nano ZnO coating (June 2015)
Notes: In June of last year, NIOSH researchers Jenny Roberts and Walter McKinney visited us to collect aerosol samples for in vivo and in vitro toxicity testing.

## Slide 22: In 2017, Dr. Jenny Roberts from NIOSH again collected dust from TiO2 painting and sanding
Notes: Dr. Jenny Roberts from NIOSH again collected dust for in vitro and in vivo toxicity testing

## Slide 23: How are we doing communicating risk to construction workers?
Question 4
1
2
3
4
Notes: Uniqueness of construction work

## Slide 24: Safe Work Australia found SDSs lacking (2010)
Evaluated 50 SDSs
18% (9/50) “were assessed as providing reliable information to appropriately inform an occupational risk assessment”
Safe Work Australia (SWA). 2010. An Evaluation of MSDS and Labels associated with the use of Engineered Nanomaterials. Commonwealth of Australia.
Notes: Source: In†the†know April†2013
The SAFENANO Team
“Safe Work Australia (SWA), an Australian national policy-setting body, carried out an evaluation of the quality of SDS for a range of nanomaterials, including metals, metal oxides, silicates and carbon nanotubes C NT) (SWA, 2010). SWA found that a large majority of the evaluated SDS (82%) presented information
that was not sufficient to fulfil an appropriate risk assessment. Moreover, many of the SDS presented data for the bulk material, without any consideration of the validity of this information for the nano form of the substance in terms of toxicology, exposure limits and control measures.”
Safe Australia evaluated 50 nano SDSs for completeness and reported that 18% (9/50) “were assessed as providing reliable information to appropriately inform an occupational risk assessment. Thus there is an urgent need for improvement.” [Safe Work Australia (SWA). 2010. An Evaluation of MSDS and Labels associated with the use of Engineered Nanomaterials. Commonwealth of Australia.

## Slide 25: CPWR surveyed 79 worker-trainers from 22 trades with an average of 30 years in the trade (2013-2014)
Survey Respondent Characteristics | N | Mean | SD | Range
Years in trade | 78 | 30.5 | 9.4 | 9-55
Years as a trainer | 79 | 13.3 | 7.8 | 1-34
Notes: Just over half of respondents were aware that nanotechnology has been applied to construction materials, but most did not know that construction products containing nanomaterials are commercially available in the USA. Only 15% of respondents reported seeing a construction nano-product in person. Of the 10 people (13%) who were aware of a nano-enabled product used on a job site, only 5 provided further detail. Three people specified aerogel insulation, one person wrote "plastering and concrete", and one person indicated that he or she could not recall the details. The remaining five people who answered yes to question 7, did not respond to the second part of the question. The vast majority of participants, almost 90%, had not addressed nanotechnology during training. Just over half of respondents were aware that nanotechnology has been applied to construction materials, but most did not know that construction products containing nanomaterials are commercially available in the USA. The vast majority of respondents reported not having seen a nanomaterial on their jobsite.

## Slide 26: Nearly half were not aware that nano had been applied to construction materials
 | Yes | No | 
Aware that nanotechnology has been applied to construction materials? | 41 (52%) | 38 (48%) | 
Aware that construction products containing nanomaterials are commercially available in the USA? | 38 (48%) | 41 (52%) | 

## Slide 27: CPWR funded a Small Study focused on nanotechnology awareness
Laura Boatman and Debra Chapman, State Building and Construction Trades Council of CA
Explore awareness among CA construction unions and employers about nano
Used questions from CPWR nano survey
Received 253 written surveys from Survey Monkey
Notes: The SBCTC represents more than 400,000 unionized construction workers in California with 175 affiliated local unions. The fact that they can draw from14 crafts means this proposed study will be able to include the majority of trades on most construction projects, which will increase the value of their findings.
In 2006, Berkeley, CA was the first US city to pass an ordinance regulating nanotechnology. Shortly after, California became the first state in the nation to pass legislation enacting a sweeping new, systematic approach to
chemical regulation with a “Green Chemistry Initiative.”
Methodology: We collected feedback from our target audience through a 31-question on-line survey and 21 follow-up key informant phone interviews with a subset of survey respondents. Our goal was to obtain 100 survey responses; we actually received 253 completed surveys to include in our evaluation. It was a priority that we obtain feedback from a cross-section of crafts. Participants were asked to identify their affiliation from a list of 25 crafts; all but one of these crafts (Pile Drivers) were represented through completed surveys. We selected 21 key informant subjects based upon one or more of the following criteria present in their survey responses: recognition of nanotechnology terms; having either received or delivered training related to nanotechnology; indicating worker and/or environmental safety concerns related to nano-enabled materials; on-the-job experience with nano-enabled construction materials; recognition of products from the eLCOSH Inventory. Interview length averaged 23 minutes (range: 9-46 minutes) per subject. Additionally, we conducted phone interviews with 5 individuals from 4 California government agencies; each interview took 30-60 minutes.

## Slide 28: “Comprehensive nanotechnology training is virtually non-existent.”
2% of respondents had received training
(Boatman and Chapman, 2018)
Notes: 1. Knowledge and Awareness: While there was far greater interest in taking this study than we originally anticipated, the level of understanding—both defining key terms and how nanotechnology may pose risks to workers in the construction industry—is quite shallow. Survey respondents and key informants voiced concern about this new technology; on the one hand respondents could see the potential benefits that nanotechnology could bring to construction, but on the other, their past experience with products like asbestos and silica make them question whether long-term consequences may exist. For many, this survey was their first introduction to nanotechnology, particularly as it might pertain to construction. The survey itself sparked in many participants an interest in learning more.
2. Knowledge of materials listed in eLCOSH Inventory: Reviewing the 500-plus product list generated interest and raised awareness of nanotechnology and could be a useful tool if used more broadly. However, given our small sample size, and the fact that some of the entries on the inventory were very generic, we really can't draw too many conclusions.
3. Current status of training: Comprehensive nanotechnology training is virtually non-existent. Barely 2% of survey participants had received training and most of these were Insulators who were being trained by a product manufacturer on proper techniques for applying the product rather than understanding the nano-enabled aspects of the material. However, the vast majority of study participants are interested in being trained about nanotechnology and believe it would be of value to construction workers.
4. Government agency monitoring, control, information: There was a surge of public sector activity around nanotechnology over the last 15 years, but this seems to have slowed now that the initial wave of funding and research has run its course. Two California agencies have the potential to gather information from nanomaterial manufacturers and make that information public, however neither is doing anything with nanomaterials at this time. They have some products on a watch list, but need more data to raise those to the action phase.
Recommendations:
A strategic plan to increase awareness and improve understanding of nanotechnology and nanomaterials in the construction industry must include a combination of research, outreach, training, and stakeholder collaboration. Information gaps need to be filled; the most basic first step is to develop clear and agreed-upon definitions of the terminology related to nanotechnology. Epidemiological data about how nanotechnology is currently being used in construction and its potential effects on workers is needed. Collaboration with public agencies, researchers, manufacturers, trainers and end-users is essential to accomplishing these goals. Additional steps include developing a multi-craft training curriculum that includes the use of video; and utilizing the eLCOSH Inventory as both an awareness tool and a way to learn more about products currently in use.

## Slide 29: Technology Safety Data Sheets may have value for advanced manufacturing
Conceived in 1994 as a tool for informing users of DOE remediation technologies about hazards
Presented at International Environmental Nanotechnology Conference, Chicago October 7, 2008
MSDSs Fail to Communicate the Hazards of Nanotechnology to Workers
Notes: Technology Safety Data Sheets (TSDSs) are novel, but untested instruments for communicating safety and health information about a new technology. As originally conceived by Matthew Fitzgerald, TSDSs would be used by workers who operate and maintain the technology, safety and health professionals charged with protecting personnel on hazardous waste sites, and regulators who must write permits for technologies on state Superfund sites.[1] The concept was presented to safety and health experts at DOE and the National Institute of Environmental Health Sciences (a part of the U.S. Department of Health and Human Services) and received sufficient interest from key actors at each organization to pursue creating a guidance document. On March 23-24, 1995, a National Technical Workshop was held in Washington, D.C. and included representatives from DOE, NIEHS, OSHA, U.S. EPA, the National Institute for Occupational Safety and Health, the U.S. Department of Defense, the Army Corps of Engineers, labor unions, universities, and private firms. The sixty participants produced a set of recommendations and agreed to gather again to produce a guidance document. On November 30th and December1st, 1995 the experts met and reached consensus on effective guidance. In October 1996, after distribution and revision of a draft, the final guidance document was issued with the first example of a Technology Safety Data Sheet (NIEHS & DOE, 1996).
A follow-up National Technical Workshop was held in Miami October 14-16, 1998 to develop more detailed guidance for considering safety and health in the design of remediation technologies. Forty-one national experts, including several from state environmental regulatory agencies, produced a draft guidance document that was revised once and issued as interim final guidelines on March 31, 1999. This document, “New Environmental Remediation Technologies: Guidance Criteria for Safety and Health” provided specific recommendations for how the key stakeholders, such as the EPA and DOE, should implement the guidance contained in the document. There was much more comprehensive guidance for creating Technology Safety Data Sheets as well.[2]
The experts at the 1996 National Technical Workshop reached a consensus that the following sections should be contained in TSDSs, in the order listed (NIEHS & DOE, p.29). [1] Dr. Fitzgerald conceived the idea while working under a contract with the Department of Energy in 1994.
[2] This document can be obtained at the Operating Engineers National Hazmat Program’s website at: http://www.iuoeiettc.org.

## Slide 30: The AIHA Nanotechnology Working Group is a valuable resource

## Slide 31: Thanks! Questions? Bruce Lippy, Ph.D., CIH, CSP Director of Safety Research blippy@cpwr.com 301-495-8527 410-916-0359 cell http://www.elcosh.org
Notes: Trainer Notes:
Try us out! Go to our site: http://www.elcosh.org or contact our Project Manager, Bruce Lippy:
Office: 301-495-8527
Cell: 410-916-0359