## Slide 1: Measurement of engineered nanomaterial exposure in microorganisms using direct and indirect methods
Monika Mortimer, Timnit Kefela, Ying Wang, Dong Li, Naresh Devarajan, Patricia A. Holden
University of California, Santa Barbara
QEEN II: 2nd Quantifying Exposure to Engineered Nanomaterials from
Manufactured Products Workshop
October 9, 2018

## Slide 2: Bioaccumulation – an important exposure-related parameter
Protozoa Tetrahymena thermophila exposed to multiwall carbon nanotubes
Uptake &
depuration rate
Longer residence time in the organism
Higher potential for harmful effects
Higher potential for trophic transfer
Carbon nanotubes
20 µm
&

## Slide 3: Microscopy and image analysis for measuring ENM uptake and depuration kinetics
Protozoa transferred to fresh medium
Exposure to 10 mg/L of nanomaterials (uptake)
Depuration
Sampling for microscopy
Image analysis

## Slide 4: How do shape and chemistry affect ENM uptake and depuration rates?
Nanomaterials (200 mg/L) were dispersed in Nanopure water with 400 mg/L alginic acid by probe sonication
Carbon black
MWCNT
Graphene
Boron nitride flakes
Boron nitride nanotubes
Carbon black
Multiwall carbon nanotubes (MWCNTs)
Graphene
Boron nitride flakes
Boron nitride nanotubes (BNNTs)

## Slide 5: Uptake and depuration kinetics results
Multiwall carbon nanotubes (MWCNTs)
Boron nitride nanotubes (BNNTs)
Graphene
Boron nitride flakes
Carbon black
x-axis: Time (h)
y-axis: ENM concentration in protozoa, mg kg-1 dw x 103
k2= 1.1 ± 0.5 h-1
k2= 0.9 ± 0.5 h-1
k2= 1.5 ± 0.9 h-1
k2= 1.6 ± 0.7 h-1
k2= 1.5 ± 0.9 h-1

## Slide 6: ENM shape-dependent depuration
Carbon black
Multiwall carbon nanotubes (MWCNTs)
Graphene
k2= 1.1 ± 0.5 h-1
Spherical food vacuoles
Polygonal food vacuoles
Fractal dimension:
1.096 ± 0.05
Fractal dimension:
1.064 ± 0.07
Fractal dimension:
1.020 ± 0.05
k2= 1.5 ± 0.9 h-1
k2= 1.5 ± 0.9 h-1

## Slide 7: Advantages of microscopy-based approach
Easy quantification of phagocytosed carbon-based ENMs
Robust comparison of uptake and depuration of different ENMs
Acquisition of both single-cell and population level information
Do not require ENM extraction from cells prior to quantification

## Slide 8: Indirect measurement of ENM exposure
20 μm
Carbon nanotubes
Pseudomonas aeruginosa exposed to 10 mg/L MWCNTs
Bradyrhizobium diazoefficiens exposed to 10 mg/L MWCNTs
MWCNT concentration, mg/L | Specific growth rate, h-1
0 | 0.46±0.02
0.1 | 0.45±0.03
1 | 0.40±0.03
10 | 0.41±0.05
MWCNTs did not inhibit bacterial growth or induce significant membrane damage
Concentration, mg/L
20 μm

## Slide 9: Omics-Based Approaches in ENM Exposure Assessment
DNA
mRNA
transcription
translation
proteins
Transcriptomics
Genomics
Proteomics
Metabolomics
metabolites
Central dogma of biology
‘Omics’ approaches

## Slide 10: Global transcriptomic response to ENMs at non-growth-inhibitory concentrations
MWCNTs
Graphene
CeO2 NPs
Carbon black
mg/L
Baceria B. diazoefficiens were grown in ENM-amended medium and gene expression was quantified using RNA sequencing

## Slide 11: Summary
Microscopy-based approach enabled easy and robust measurement of ENM uptake and depuration kinetics.
Tubular ENMs had longer residence times in protozoa, thus may have a higher potential for harmful effects and trophic transfer.
Non-targeted ‘omics approaches are promising in developing biomarker-based methods for indirect ENM exposure assessment.

## Slide 12: Acknowledgements
Prof. Patricia Holden (UCSB) &
the Holden Lab members:
Timnit Kefela, PhD student
Anne Trinh, undergrad. student
Ying Wang, PhD candidate
Dr. Dong Li
Dr. Naresh Devarajan
Bren School of Environmental Science & Management, UCSB